## D. ADAM & ASSOCIATES

#### Making the Difference with ACTEL products

Armaglaze Permanent Anti-Graffiti Coating – Graffiti Removal

Method Statement and Technical application notes

PRODUCT USE:

ARMAGLAZE is highly resistant to solvents and to u.v. radiation. Subsequent damage from graffiti is unable to soften and penetrate the dried ARMAGLAZE film. Graffiti is easily removed by aromatic & aliphatic solvent based graffiti removers on a brush or spray on, agitate, wipe away basis, repeatedly without damage to ARMAGLAZE.

GRAFFITI REMOVAL:

Graffiti is removed from ARMAGLAZE protected surfaces as follows:

- Apply ACTEL’s Come Clean or other solvent based graffiti removers by brush, starting from the bottom and working upwards.

- Allow appropriate contact time for the graffiti binders to soften and break up

- Agitate with a bristle brush, deck scrubber etc. to help break down graffiti solids

- Wipe residues away with rags, turning them frequently.

- Most graffiti removers are water rinsable. After their use, wash down the area being cleaned with a water based hard surface cleaner or neutral detergent to remove all solvent and graffiti residues.

- Cleaning should be carried out in square metre blocks, finishing one block before starting the next.

- DO NOT use paint strippers. These usually contain methylene chloride (dichloromethane) which can damage the ARMAGLAZE film.

- For stubborn stains, add talc to graffiti remover to make a paste and poultice the stained area overnight, covered by black plastic sheet. Remove poultice solids with a wooden spatula and rinse off any residues.

Winter conditions: In winter conditions, graffiti removal is slowed by cold temperatures. In tropical temperatures, protect work areas with sheeting or black plastic to prevent too rapid evaporation of graffiti removal solvents.

HEALTH & SAFETY CONSIDERATIONS:

Always follow the Health & Safety precautions given in manufacturers’ Material Safety Data Sheets particularly for solvent based products and store solvents securely & safely

For personal protection, wear safety glasses to protect the eyes from splashes, and

protect skin and hair with coveralls, gloves, cap or hard hat.

In confined areas ensure that there is adequate ventilation to dispel solvent fumes.

Do not allow smoking in the work area.

Restrict public access to work areas.

D. Adam & Associates, Clarendon, High Cross Avenue, Melrose TD6 9SQ  Scotland

Tel: +44 1786 472465 / 7880805478 E-mail: dougadam@globalnet.co.uk www.actel.f9.co.uk

D. Adam & Associates is approved to apply ACTEL Coatings products.