ACTEL Coatings

Clarendon, High Cross Avenue,

Melrose TD6 9SQ Scotland

Tel:  +44 (0) 7880 805478

E-Mail: dougadam@globalnet.co.uk

URL: www.actel.f9.co.uk

Clarendon, High Cross Avenue,

Melrose TD6 9SQ

Tel:  +44 (0) 7880 805478

E-Mail: dougadam@globalnet.co.uk

URL: www.actel.f9.co.uk

ENVIROGUARD

The environmentally safe facade protection system.

Buildings made of brick, stone and concrete are constantly subjected to the damaging influences of weathering, dirt and air borne chemical pollution.

The resulting damage costs £ billions each year, costs which are escalating rapidly. Added to these costs is the cost of damage from spray paints (graffiti) which can be extremely difficult to remove, especially from unprotected stone and brickwork.

The authorities responsible for building maintenance, restoration and conservation, only take notice when they become aware of the enormous sums of money which are spent yearly in repairing buildings and monuments which have deteriorated rapidly as a result of these influences.

Until now, there were few measures available to prevent this costly damage. Commonly used cleaning practices, traditionally based on the use of dangerous acids, caustic cleaners or chlorinated solvents, have not always been friendly to the environment or to the employees involved in applying them.

With ENVIROGUARD it is now possible to undertake preventative measures at a relatively low cost both in terms of financial cost and environmental impact.

The ENVIROGUARD system was developed with the following properties

-  single component system.

-  EASY AND SAFE TO USE.

-  FRIENDLY TO THE ENVIRONMENT.

-  NEUTRAL INVISIBLE FILM.

-  PROTECTIVE HYDROPHOBIC PROPERTIES.

-  REVERSIBLE , EASY TO REMOVE.

ACTEL Coatings

Clarendon, High Cross Avenue,

Melrose TD6 9SQ Scotland

Tel:  +44 (0) 7880 805478

E-Mail: dougadam@globalnet.co.uk

URL: www.actel.f9.co.uk

ENVIROGUARD

The environmentally safe facade protection system

The Products

Enviroguard 					Weather proofing building treatment

Enviroguard Anti-Graffitti 			Water based graffiti protection

Enviroguard Fly Away 				Protects against fly posting

## Enviroguard CGR					Prevents chewing gum adhering

Preparation of the surface.

The surface must be clean and in perfect condition. Constructional defects such as

crevices, cracked joints, faulty connections, rising damp and hygroscopic moisture

must be eliminated before treatment begins. It must be ensured that water and harmful salts that are dissolved in the water do not penetrate behind the zone to be treated.

Prior to treatment adherent crusts of pollutants and contaminants as well as blooms,

algae and moss, must be treated and removed. The opening up of surface pores and capillaries during this preparatory cleaning, will ensure that a satisfactory uptake and absorption of  ENVIROGUARD is achieved. During cleaning , care must be taken to ensure that building surfaces are subjected to as little damage as possible.

Residues from the cleaning process may effect the efficiency of the ENVIROGUARD system  and must therefore be removed completely.

Quality of the surface.

If harmful salts such as sulphates, chlorides and nitrites exist, a quantitative analysis of

these salts may be necessary. High concentrations of harmful salts lead to constructional damage which cannot be put right by ENVIROGUARD treatment.

Adjacent surfaces.

Mask off any areas, doors, windows etc. adjacent to surfaces specified for ENVIROGUARD  protection  to avoid accidental coating.  Any overspray or spillage should be washed freely with water before being allowed to dry, taking care not to wet areas covered correctly.

Tools and equipment.

ENVIROGUARD products are ready to use for air assisted or airless spray application but may be diluted for use with low pressure back pack sprayers all of which are suitable as application equipment. All  tools must be kept clean and dry before use. After use or prior to prolonged work stoppages, tools and particularly spray tips, must be thoroughly cleaned with water.

ACTEL Coatings

Clarendon, High Cross Avenue,

Melrose TD6 9SQ Scotland

Tel:  +44 (0) 7880 805478

E-Mail: dougadam@globalnet.co.uk

URL: www.actel.f9.co.uk

ENVIROGUARD

Profile of product properties.

ENVIROGUARD is a water based, micro emulsion used for protecting building surfaces from attack by erosion and atmospheric pollution and as a primer for Enviroguard Anti-Graffiti.

ENVIROGUARD  treatment is reversible - the system can be removed preferably by low pressure washing (max. 1200 psi for stone) with hot water (850C) or by Envirogel with cold water washing .

ENVIROGUARD  imparts very strong hydrophobic properties to protected surfaces whilst the micro porous nature of the treatment still allows the building to “breathe”.

ENVIROGUARD  permits easy future cleaning of treated buildings using only water.

Field of Application

ENVIROGUARD  can be used for the treatment of all mineral building materials such as sandstone, limestone, brick, plaster and concrete. It can safely be used for the treatment of sculptures and monuments.

ENVIROGUARD  will also impart waterproof and fungicidal properties to surfaces which have been coated with emulsion paint.

Product application and processing

ENVIROGUARD  is designed to be applied to building surfaces by airless spray, or low pressure flow coating. The material should be applied by low pressure or pump sprayer so that the liquid film runs 30 to 50 cms down the surface of the building material being treated.

It is possible to apply the product by brush or roller but application by airless sprayer in two or three coats always gives best results.

Suggested product coverage rates

Clinker		5 - 10  m2/lt.			Granite		6 - 10   m2/lt.

Limestone		3 - 5	  m2/lt.			Concrete		3 - 5     m2/lt.

Sandstone		3 - 8    m2/lt.			Plaster		3 - 5	   m2/lt

Brick			6 - 10  m2/lt.			Painted masonry    10 -12   m2/lt.

ACTEL Coatings

Clarendon, High Cross Avenue,

Melrose TD6 9SQ Scotland

Tel:  +44 (0) 7880 805478

E-Mail: dougadam@globalnet.co.uk
URL: www.actel.f9.co.uk

ENVIROGUARD ANTI-GRAFFITTI

Profile of product properties.

ANTI-GRAFFITTI is a water based, micro emulsion used for protecting building surfaces from damage by spray paint and marker pens.

ANTI-GRAFFITTI  treatment is reversible, the system can be removed, along with any graffitti markings, by pressure washing with hot water (850C) or with Envirogel and cold water.

ANTI-GRAFFITTI is a sacrificial treatment which gives added protection to vulnerable building areas from attack by graffitti vandals.

ANTI-GRAFFITTI provides an effective anti-graffitti barrier to protected surfaces whilst the micro porous nature of the treatment still allows the building to “breathe”.

Field of application.

ANTI-GRAFFITTI  can be used to protect all mineral building materials such as sandstone, limestone, brick, plaster and concrete which have been pre-sealed with one or two coats of ENVIROGUARD.

It can also be used to protect surfaces painted with emulsion paint from graffitti attack.

Product application and processing

ANTI-GRAFFITTI coating should be applied by brush or roller to surfaces which have been previously treated with ENVIROGUARD .

ANTI-GRAFFITTI may be applied by airless spray or may be diluted up to 20% with clean water for application by low pressure knapsack sprayer.

For use on untreated surfaces consult the manufacturer’s product literature.

Removal of graffitti.

Graffitti damage can easily be removed from treated surfaces by washing down the surface with a hot water (85oC)  pressure  wash. The protective coating is removed along with the graffitti. The product should then be reapplied to cleaned areas.

Suggested product coverage rates

10  m2/lt  when applied onto smooth surfaces pre-sealed with ENVIROGUARD.

ACTEL Coatings

Clarendon, High Cross Avenue,

Melrose TD6 9SQ Scotland

Tel:  +44 (0) 7880 805478

E-Mail: dougadam@globalnet.co.uk

URL: www.actel.f9.co.uk

ENVIROGUARD FLY AWAY

Profile of product properties.

FLY AWAY  is a formulation of  waxes dissolved in white spirit, used to protect building surfaces, street furniture and road signs from contamination by unwanted bills or posters.

FLY AWAY  treatment is reversible, the system can be removed by washing the surface with white spirit or washing the surface with white spirit or suitable emulsifiable solvent degreasers and pressure washing with hot water (850C).

FLY AWAY  causes unwanted posters to fall off and “fly away” from treated surfaces.

FLY AWAY  also provides an effective waterproof  barrier which gives added anti-rust protection to painted metal street fittings which are subject to damage by road salts.

Field of application.

FLY AWAY  can be used to protect all mineral building materials such as sandstone, limestone, brick, plaster and concrete which have been pre-sealed with ENVIROGUARD .

Most surfaces which are capable of being painted can be kept free from bills and fly posters by coating with FLY AWAY .

Product application and processing

FLY AWAY  coating should be applied by brush or roller to natural building surfaces which have been previously treated with ENVIROGUARD, to ensure the low visibility of the product.

For other non porous surfaces a single coat of FLY AWAY  will give the required protection against fly posting.

Removal of fly posters.

When the adhesive holding the fly poster dries out,  the poster will fall to the ground under the effects of natural weathering.

Suggested product coverage rates

6/8 m2/lt  when applied by brush or roller to surfaces pre sealed with ENVIROGUARD .

10/12 m2/lt when applied to non porous surfaces.

ENVIROGUARD CGR

Profile of product properties.

ENVIROGUARD CGR is a water based, micro emulsion used to stop chewing gum adhering strongly to paved areas, making it quick and economical to remove.

ENVIROGUARD CGR treatment is reversible - the system can be removed preferably by low pressure washing (max. 1200 psi for stone) with hot water (850C) or by Envirogel with cold water washing.

ENVIROGUARD CGR imparts very strong hydrophobic properties to protected surfaces whilst the micro porous nature of the treatment still allows surfaces to “breathe”.

ENVIROGUARD CGR permits easy future cleaning of treated pavements using only low pressure water washing.

ENVIROGUARD CGR allows paved pedestrian walkways to be cleaned free of gum without loss of the sand used to bed in the block paving.

Field of Application

ENVIROGUARD CGR can be used for the treatment of all mineral building materials such as sandstone, limestone, brick, and concrete.

ENVIROGUARD CGR will also impart waterproof and fungicidal properties to surfaces which have been treated.

Product application and processing

ENVIROGUARD  is applied by pump sprayer. The material should be applied at low pressure with a fan spray in two coats.

It is possible to apply the product by brush or roller but application by sprayer in two or three coats always gives best results.

Suggested product coverage rates

Clinker		5 - 10  m2/lt.			Granite		6 - 10   m2/lt.

Limestone		3 - 5	  m2/lt.			Concrete		3 - 5     m2/lt.

Sandstone		3 - 8    m2/lt.			Brick			6 - 10  m2/lt.

ACTEL Coatings

# E-Mail: dougadam@globalnet.co.uk    http://www.actel.f9.co.uk