ACTEL Coatings-Making the Difference

STEEL PROOF - Frequently Asked Questions

Q. What is Steel-Proof?

A. Steel-Proof is a heavy duty rust preventative compound for clean, bare or painted steelwork which dries to give a semi-hard finish.

Q. How do you use it?

A. Make sure that surfaces are clean and paintwork Is sound. Then you can apply Steel-Proof by brush or roller.

Q. How many coats do you need?

A. Steel-Proof is a one coat product.  However, the best results are achieved by applying coats of 1 mil thick.

Q.  WHat is the difference in performance between one coat and two coats of Steel-Proof?

A. Depending upon how severe the conditions are, one full, thick coat lasts from 2 to 5 years.

Q. Can you apply Steel-Proof to blast cleaned steel?

A. Yes if there is to be a period of prolonged storage of the prepared steel.

Q. On what surfaces is it used?

A. Steel-Proof is used on iron and steel structures and on non-ferrous metalwork.

Q. Will Steel-Proof stop rust?

A. Yes, Steel-Proof is an outstanding rust preventative.

Q. Will the product freeze?    A.  No

Q. How quickly does Steel-Proof dry?

A. Tack dry in 1 to 2 hours.

Q. Can I paint over Steel-Proof?

A. No. Steel-Proof is a stand alone rust preventative.

Q. Can I use Steel-Proof if it is damp or humid outside?

A. Yes. Steel-Proof can be used in damp humid conditions. Surfaces which are wet should be protected with Steel-Proof DW Grade.

Q.  What happens if it rains on treated surfaces before Steel-Proof dries?

A. Steel-Proof is not affected by rain even immediately after application.

Q. Can I use Steel-Proof in Ultra High Pressure Blasting specifications? A.   Yes, so long as it is DW Grade.

Q. What is Steel-Proof made of?

A.  Steel-Proof is a spirit based blend of calcium sulphonates, waxes and additives.

Q. Is Steel-Proof resistant to saltwater or road salts?

A. Yes. Steel-Proof is exceptionally resistant to salt and passes 1100 hours salt fog test when applied at minimum 1.00 mil dry film thickness.

Q. How does the product work?

A.  Steel-Proof’s dry film exhibits a unique plate like interleaving “fish scales” structure to impede the passage of moisture through the protective film.

Q. Does it have uses other than rust prevention?

A. Yes. It provides a very flexible coating to protect plant and equipment in transit and in assembly.

Q. Does it come in colours?

A. No. The product dries tan, translucent brown.

Q. Is Steel-Proof removable?

A. Yes. When protection is no longer required, Steel-Proof is removed using solvent degreaser and hot water.

Q. Must it be removed?

A. Not at all. Residual Steel-Proof acts as an initial lubricant when plant is brought back into use.

Q. Is the product harmful or is it hazardous?  A. Not at all.

Q. Does the product smell?

A. Steel-Proof has a faint characteristic smell.

Q. Is the product environmentally safe?

A. The product is engineered to be as environmentally “friendly” as possible.

Q. Is Steel-Proof flammable. A. Yes. Flash point is 40oC

Q. What happens if I get it on my hands?

A. Wash off with soap and water. It is always good practice to wear gloves when applying coatings.

Q. What do I do if it gets on my clothes?

A. wash affected area with soap and water before it dries. Dry cleaning clothes will also remove Steel-Proof.

Q. What first aid is required?

A. Splashes on skin or eyes should be flushed well with water.

Q.  What about cleaning up after use?

A. Use paint thinners to clean equipment before Steel-Proof dries and aromatic solvents if it has dried.

Q. What will happen if I apply Steel-Proof on a hot surface?

A. Heat will soften the coating. It will harden again when cool. However, Steel-Proof will not slump below 107oC nor will it burn when flame source is removed.

Manufactured for world markets only by:

ACTEL Coatings

Clarendon, 17 High Cross Avenue,

Melrose TD6 9SQ Scotland U.K.

Tel:/Fax: +44 (0) 7880 805478

E-mail: dougadam@globalnet.co.uk

Web site:  http://www.actel.f9.co.uk