TECCPROF.DOC Page 1 of TECHNICAL DATA SHEET.

1.	IDENTIFICATION OF PRODUCT AND COMPANY

1.1	Product name : 	 CRETA-SEAL

Water based invisible permanent sealer to harden

waterproof and dust proof new or old concrete.

1.2	Company        :  D. Adam & Associates / ACTEL Coatings

Clarendon, 17 High Cross Avenue, Melrose TD6 9SQ Scotland, U.K.

Tel: +44  (0) 7880 805478  E:  dougadam@globalnet.co.uk    www.actel.f9.co.uk

2.	TECHNICAL DATA

2.1	STORAGE:		Store securely in original sealed containers. Frozen product can be 				thawed, stirred well and still used safely.

2.2	APPLICATION:	Apply two or three coats by low pressure spray, brush or roller.

Brush out ponding. See separate specification notes for full 					application details.

2.3	COVERAGE:		Theoretical  - 25 litres treats 145sq. Mts in 3 coats

Max. Penetration - 1.00 to 1.50 cms (0.4-0.5 inches)

2.4	PACK SIZE:		25 litre or 200 litre drums.

2.5	FLASH POINT:		None.

2.6	FIRE RESISTANCE: 	Not tested. Not flammable under any conditions.

2.7	TOXICITY:		Non toxic.

3.	PREPARATION

3.1	Stir well before use.

3.2	Concrete should be clean and free from surface dirt, dust and grease. CRETA-SEAL

should not be applied over existing coatings. It is intended for absorption into cracks, pores and air holes in concrete where it acts as a strengthener and sealer with good hydrostatic properties. If coatings have broken down and CRETA-SEAL is specified as part of the renovation work, all coatings must first be removed. Surfaces need not be dry.

3.3	Temperatures should be above 42oF and below 125oF and application should not be

attempted if lower temperatures are forecast during the application period.

3.4	Remove all mould growth in damp floors and walls in cellars etc.by washing thoroughly.

3.5	Cured concrete floors should be cleaned with a strong stripper a 7:1 solution of Muriatic

acid for example and or a strong detergent e.g. TSP to remove any existing organic surface layer.

TECCPROF.DOC Page 1 of 2

4.	APPLICATION

4.1	CRETA-SEAL should be stored at room temperature (20oC/68oF) for 24 hours before use.

4.2.1	Apply to new concrete as soon as the water sheen has gone and the floor can be walked

on.

4.2.2	Vertical formed concrete structures can be treated as soon as the forms are taken down.

4.3	Dilution rates:	First Coat: 	1 part Creta-Seal  + 4 parts clean water

Second Coat:	1 part Creta-Seal  + 3 parts clean water

Third Coat :	1 part Creta-Seal  + 2 parts clean water and any further 						coats.

After dilution, stir well before applying by brush, roller or low pressure spray to saturate 	concrete surfaces. Application in three coats of increasing solids content gives maximum 	penetration of Creta-Seal into concrete capillaries. (Creta-Seal can also be applied

undiluted in a single application with periodic wetting over with water spray followed by use of a squeegee to remove surface wet product until Creta-Seal has been fully absorbed into the concrete).

4.4	Avoid ponding. Brush out or squeegee away any excess of CRETA-SEAL. Avoid over 	saturation.

4.5	When dry and within 16 hours of application, rinse work area with water to speed up 	sealing reaction and remove any excess leaching of soluble salts.

4.6	When surface dry, repeat the application.

4.7	If excessive leaching is experienced, continue washing to rinse away excess salts and 	contaminants until the leaching stops, usually within 3  to 7 days.

4.8	Third coat test: After the proper application of two coats of CRETA-SEAL a simple test

for the 	need or otherwise for a third application can be carried out by taping down several pieces of  foam rubber or sponge to the concrete deck. If after 24 hours, either the sponge or the concrete surface is wet, a third application is necessary.

5. 	LIMITATIONS

5.1	CRETA-SEAL should not be left on glass, glazed surfaces or aluminium.

5.2	Some bricks have a composition which can cause the leaching of excessive alkali and 	efflorescence after treatment with CRETA-SEAL. If this occurs, hose down periodically to 	avoid surface staining.

5.3 	CRETA-SEAL should not be applied at a product temperature of less than 42oF.

6.	HEALTH AND SAFETY

These products are considered to be non hazardous. However, please ensure that

operators read and understand the health and safety data sheet before using these materials.

Revised May 1999