TECCLEARWAY.DOC Page 1 of2 TECHNICAL DATA SHEET.

1.	IDENTIFICATION OF PRODUCT AND COMPANY

1.1	Product name : 	 FACAIDE~525

Water based invisible 10 year sealer for concrete and stone

facades. Treated surfaces become highly water resistant and

resistant to acid gases, remaining clean with natural

weathering

1.2	Company        :  D. Adam & Associates / ACTEL Coatings

Clarendon, 17 High Cross Avenue, Melrose TD6 9SQ Scotland, U.K.

Tel: +44  (0) 7880 805478  E:  dougadam@globalnet.co.uk    www.actel.f9.co.uk

2.	TECHNICAL DATA

2.1	STORAGE:		Store securely in original sealed containers. Store at temperatures

between 5 and 40oC

2.2	APPLICATION:	Apply one saturation coat by low pressure spray, brush or roller.

Brush out ponding. For porous surfaces i.e. greater than 15%, a
                                              second application may be needed. Test surfaces first in order to
                                              establish the correct material requirement.

2.3	COVERAGE:		Theoretical  - 200 gms per sq metre

Max. Penetration - 1.00 to 1.50 cms (0.4-0.5 inches)

2.4	PACK SIZE:		5, 25 or 200 litre drums.

2.5	FLASH POINT:		None.

2.6	FIRE RESISTANCE: 	Not tested. Not flammable under any conditions.

2.7	TOXICITY:		Non toxic. For excessive use, wear protective clothing, eye shield

and respiratory mask protection

3.	PREPARATION

3.1	Stir well before use.

3.2	Surfaces should be clean and free from surface dirt, dust and grease. FACAIDE~525

should not be applied over existing coatings. It is intended for absorption into cracks, capillaries and air holes in concrete where it acts as a long term sealer with good hydrostatic properties. If coatings have broken down and FACAIDE~525 is specified as part of the renovation work, all coatings must first be removed. Surfaces need not be dry.

3.3	Temperatures should be above 42oF and below 125oF and application should not be

attempted if lower temperatures are forecast during the application period.

  - Remove all mould growth and surface contaminants by power washing thoroughly. If acid

cleaning is used, rinse well and neutralise surfaces before application begins

TECCLEARWAY.DOC Page 2 of2

4.	APPLICATION

4.1	FACAIDE~525 should be stored at room temperature (20oC/68oF) for 24 hours before use.

4.2.1	Apply to new concrete as soon as the concrete is “green”

4.2.2	Vertical formed concrete structures can be treated as soon as the forms are taken down.

4.3	Stir well before applying by brush, roller or low pressure spray to saturate	concrete
            surfaces working from top to bottom on vertical surfaces. FACAIDE~525 should be applied

undiluted in a single application to flood the area to be treated. For sound concrete, that is

at a rate of 1 litre of FACAIDE~525 per 5 sq metres.

4.4	Avoid ponding. Brush out or squeegee away any excess of FACAIDE~525. Avoid over 	saturation.

5. 	LIMITATIONS

  - FACAIDE~525 should not be left on glass, glazed surfaces or aluminium. Mask these

areas prior to application.

5.2	Some bricks have a composition which can cause the leaching of excessive alkali and 	efflorescence after treatment with FACAIDE~525. If this occurs, hose down periodically to 	avoid surface staining.

5.3 	FACAIDE~525 should not be applied at a temperature of less than 42oF.

6.	HEALTH AND SAFETY

These products are considered to be non hazardous. However, please ensure that

operators read and understand the health and safety data sheet before using these materials. For spray application, suitable filter masks should be used to protect the nose and mouth against ingesting spray particles

Revised February ‘04