TECHNICAL DATA SHEET. 		TECHGLZF.DOC Page 1 of 4

1.	IDENTIFICATION OF PRODUCT AND COMPANY

1.1	Product name : 	ARMAGLAZE TOPCOAT

Heavy duty permanent architectural and anti-graffitti coating

1.2	Product type:		Superior quality 2-pack aliphatic polyurethane coating

1.3	 Company        :  D. Adam & Associates / ACTEL Coatings

Clarendon, 17 High Cross Avenue, Melrose TD6 9SQ Scotland, U.K.

Tel: +44  (0) 7880 805478  E:  dougadam@globalnet.co.uk    www.actel.f9.co.uk

2.	TECHNICAL DATA

2.1	STORAGE:		Store securely between 10oC and 20oC

2.2	APPLICATION:		Application should be by competent, trade applicators 						experienced in 2-pack industrial coatings.

Apply two coats by spray, brush or roller to surfaces already  					sealed or painted. Bare concrete should be sealed with 						ARMAGLAZE SEALER or ARMAGLAZE WRE SEALER.

New steelwork should be primed with a good anti-corrosion primer.

On non-porous, hard smooth surfaces, it is necessary to abrade the 				surface first to improve adhesion.								Airless spray tip sizes: 0.011 to 0.021 inches.

2.3	OVERCOATING:	ARMAGLAZE should be overcoated after 8 hours and within 24 					hours. After 24 hours, ARMAGLAZE needs flatted down by abrasive 				sanding before applying a final coat.

2.4	DRYING TIME:		4 to 8 hours.

2.5	COVERAGE:		Theoretical - to   10 sq. Metres per litre.

Practical     - 6 - 10 sq. Metres per litre.

2.6	DRY FILM:		28  microns per coat.

2.7	VOLUME SOLIDS:	65 - 80 % depending upon pigmentation

2.8	PACK SIZE:		2 pack product, 6 kilos of product when mixed

2.9	MIXING RATIO:	2.25 parts Resin Base Pack A : 1 Part Curing Agent Pack B

2.10	FLASH POINT:	 	38oC

2.11	FLAME SPREAD:	Tested to Class 1 on porous, plasterboard. Manufactured to meet 				Class “O” on metal and other non-porous, non-combustible surfaces.

2.12	TEMPERATURE 	105oC/221o F continuous, 200-250oC/392oF-482oF for short 		RESISTANCE:		spells. Coating is thermoplastic.

2.13	APPEARANCE:	Available in Clear and full BS 4800 colour range, full or semi	 				gloss and matt finish. Full gloss finishes are most resistant to dirt.

2.14	TOXICITY:		Non toxic pigmentation, inert in dried film

TECHGLZF.DOC Page 2 of 4

3.	PREPARATION

3.1	Read the Material Safety Data Sheet before use.

3.2	Surfaces should be clean and free from surface dirt, dust, grease, wax and millscale.

3.3	All loose friable material should be removed and damaged areas made good.

3.4	Efflorescence, laitence and mould growth should be removed and treated as appropriate.

3.5	Graffitti marks remaining after preparation can be obliterated under two coats of 	ARMAGLAZE TOPCOAT Colour, and need not be totally removed.

3.6	Work in progress must be protected by contractors both from adverse weather and physical 	damage before use.

4.	APPLICATION

4.1	Mix ARMAGLAZE Pack B Curing Agent thoroughly into ARMAGLAZE Pack A and let	stand for 15-20 minutes before using.

4.2	Test compatibility on existing paint by applying ARMAGLAZE to a small inconspicuous area 	and observing that there is no wrinkling, blistering or discolouration.

4.3	If in doubt, strip back to bare surfaces and re-seal with ARMAGLAZE PRIMER or 	ARMAGLAZE WRE SEALER. (Always use WRE SEALER to patch seal broken painted 	areas before using ARMAGLAZE TOPCOATS).

4.4	Apply ARMAGLAZE when the air and surface temperature is above 5oC and the relative 	humidity between 40% and 80%. Cold conditions or condensation may adversely 	affect the appearance of the dried film.

4.5	For brush and roller applications, it is important to achieve a smooth, even coating. Add 5% 	to 10% ARMAGLAZE THINNERS in small additions to improve “wet edge” time and flow 	properties.

4.6	Do not 	overload brushes and rollers with excessive amount of product so as to cause runs 	or ponding. ARMAGLAZE is a thin film product with a very hard, dense surface finish.

4.7	Use short pile, solvent resistant rollers for smooth surfaces.

4.8	After applying by roller, lay off by brush for an even finish.

4.9	Brushing or rolling should not be so vigorous as to cause air entrapment.

4.10	For spray work, apply by airless or air assisted sprayers in evenly applied fine mist coats 	thinned as necessary with up to 15% ARMAGLAZE THINNERS. Apply the second coat at 	right angles to the first. Take care to cover all of the surface irregularities and indents.

4.11	Apply at the recommended coverage rates.

TECHGLZF.DOC Page 3 of 4

5.	GRAFFITTI REMOVAL & SURFACE CLEANING

5.1	Because ARMAGLAZE is strongly solvent resistant, graffitti damage does not penetrate the 	dried film. Removal of graffitti using strong solvents with no damage to the protective coating 	is therefore a simple task. Surface grime can be removed by washing down with detergent 	and water.

  - Graffitti damage should be cleaned off using absorbent cloths or scrubbing brushes wetted with CLEANAWAY GTi, an environmentally safer, water miscible graffitti remover,

ARMAKLEEN an aliphatic solvent based graffiti remover or any of the many commercially

available solvents and graffitti removers on the market.

5.3	It may be necessary to repeat the graffitti removal process for stubborn markings.

“Shadows” left after cleaning dye marker pens can be removed using methanol or 	 “OUTLINE”.

5.4	DO NOT USE METHYLENE CHLORIDE BASED PAINT STRIPPERS.

5.5	Wear eye protection and solvent resistant gloves when using graffitti removers.

6. OTHER TECHNICAL and TEST DATA

6.1	FREE ISOCYANATE:	When mixed Pack A+B, ARMAGLAZE has no measurable free 					isocyanate at standard room temperature and pressure (STP).

6.2	SALT FOG RESISTANCE: (ASTM B-117 & ASTM D-714)  10,000 hours

6.3	ACID RAIN HUMIDITY:	(Kesternich Test)	30 cycles

6.4	ABRASION & EROSION

RESISTANCE		(ASTM D-968)  251 per mil

6.5	GLOSS RESISTANCE:	 South Florida Testing Service for 48 months 51%

6.6	BEND (ASTM D522):	The film started cracking at 14% elongation. After 1000 hours the 				film started cracking at an elongation of 3%.

6.7	HARDNESS 		The paint had a hardness of H/HB.

(ASTM D3363):		After artificial weathering  the film had a scratch hardness of H/HB

6.8	TABOR ABRASER	Weight loss after	Weight loss after

(ASTM D4060):		500 cycles		1000 cycles

Panel A:		0.0246g		0.0539g

Panel B:		0.0242g		0.0481g

6.9	SCRUB RESISTANCE:	No effect on paint film after 1500 cycles, other than slight marring of 				the finish by the nylon brush

6.10	IMPACT (BS3900:E3):	There was no cracking or loss of adhesion with a 1.0 mm indentation 				direct impact.

TECHGLZF.DOC Page 4 of 4

6. OTHER TECHNICAL and TEST DATA Cont’d.

6.11	ADHESION:		(ASTM D3359)    5B

6.12	ARTIFICIAL WEATHERING: (1000 hours)  No chalking occurred and the panels lost only

(ASTM-G53)		4 gloss units from 60 degrees average of 89 to 85. The scratch 					hardness of the paint was not affected but the flexibility deteriorated.

6.13	SO2 RESISTANCE:	The panels were not affected after 10 cycles

6.14	HOT SALT SPRAY:	(ASTM B117)  1000 hours no visible effect

6.15	SOLVENT RESISTANCE:(BS 3900) G5 method. The paint film was unaffected by 1/2 hours 				immersion in Xylene, M.I.B.K. or M.E.K.

6.16	INTERNAL STRESS:	The internal stress of the paint film is negligible.

6.17	SHELF LIFE:		12 months minimum at recommended storage temperatures in 					original sealed containers.

6.18	EQUIPMENT CARE:	Clean all spray equipment immediately with ARMAGLAZE 					THINNERS. After use, brushes and rollers may not be reusable.

7. HEALTH AND SAFETY

Please ensure that operators read and understand the health and safety data sheet 	before 	using ARMAGLAZE. Particularly where application is by sprayer, follow the 	requirements for personal protection including use of respiratory protection.

Revised May 1999