TECHBEST.DOC Page 1 of 2

TECHNICAL DATA SHEET.

1.	IDENTIFICATION OF PRODUCT AND COMPANY

1.1	Product name : 			BEST-O-SEAL

Water based sealer / encapsulant for asbestos etc.

1.2	Company        :  D. Adam & Associates / ACTEL Coatings

Clarendon, 17 High Cross Avenue, Melrose TD6 9SQ Scotland, U.K.

Tel: +44  (0) 7880 805478  E:  dougadam@globalnet.co.uk    www.actel.f9.co.uk

2.	TECHNICAL DATA

2.1	STORAGE:	Water based product, protect from freezing.

2.2	APPLICATION: Apply one or two coats by spray, stiff brush or roller to seal
                          porous surfaces, provide a vapour barrier or bind and encapsulate
                          friable asbestos.

2.3	OVERCOATING:	8 hours if overcoating with a water based product, allow up to
                                              24 hours if overcoating with solvent based materials. Best-O-
                                              Seal discolours in U.V. light and should be overcoated if a 				decorative finish is required.

2.4	DRYING TIME:	2 to 4 hours, very dependent on the drying conditions.

2.5	COVERAGE:		Theoretical  - up to 12 sq. Metres per litre.

Practical      - 4-10 sq. Metres per litre.

2.6	PACK SIZE:		25 litre or 200 litre drums.

2.7	DRY FILM:		25 microns when applied at 50 microns wet film thickness

2.8	FLASH POINT:	None.

2.9	VISCOSITY:		30 seconds Ford 4 Cup at 20oC

2.10	TOXICITY:		Non toxic and inert dry film

TECHBEST.DOC Page 2 of 2

3.  PREPARATION

3.1	Best-O-Seal is supplied ready to use. Stir well before use. First coat may be

thinned with 5% clean water. Subsequent coats should be applied without thinning.

3.2	Surfaces should be clean and free from mould, surface dirt, dust and grease.

3.3	Porous and friable asbestos surfaces, should be damped down with a fine water

spray mist before application to prevent disturbance of loose fibres. Best-O-Seal can then be applied to the damped down surface although initial drying will be slower.

4.	APPLICATION

4.1	Best-O-Seal should be stored at room temperature (20oC/68oF) for 24 hours before

use. Do not allow to freeze.

4.2	Apply Best-O-Seal when the air and surface temperatures are between 5oC and

30oC and the relative humidity between 40-90%.

4.3	Two coats applied by brush is the preferred specification. A third coat may
            be necessary on more porous surfaces. Best-O-Seal can be spray applied to larger
            areas.

4.4	Best-O-Seal in the wet state is off white in colour. It dries clear with a tendency to

discolour where exposed to daylight.

4.5	Best-O-Seal will normally be touch dry within 30 to 60 minutes  hours depending on
            temperature and humidity. Cooler temperatures delay curing. Allow up to 8 hours
            before overcoating with water based products and up to 24 hours with solvent
            based topcoats.

4.6	Wash brushes and equipment with water immediately after use. Clean spray lines

before 	Best-O-Seal dries. Once dry, Best-O-Seal is difficult to remove. Use an aromatic solvent to soften dry brushes or free clogged lines.

5.	HEALTH AND SAFETY

5.1	These products are considered to be non hazardous. However, please ensure that

operators read and understand the health and safety data sheet before using these materials.

5.2	Asbestos removal or encapsulation is a specialist process and should be

undertaken only by experienced trained operatives familiar with the relevant Health & Safety and Local Authority regulations.

Revised May 1999