TECHNICAL DATA SHEET. 		TECHENVD.DOC Page 1 of 2

1.	IDENTIFICATION OF PRODUCT AND COMPANY

1.1	Product name : 	ENVIROGUARD

Water based sacrificial building protection coating

1.2	Company        :  D. Adam & Associates / ACTEL Coatings

Clarendon, 17 High Cross Avenue, Melrose TD6 9SQ Scotland, U.K.

Tel: +44  (0) 7880 805478  E:  dougadam@globalnet.co.uk    www.actel.f9.co.uk2.	TECHNICAL DATA

2.1	STORAGE:		Protect from freezing.

2.3	APPLICATION:		For light to moderate protection, apply a minimum of three coats by 				by spray, brush or roller.

2.4	OVERCOATING:	Enviroguard can be applied in mist coats, wet on wet. 						Otherwise, recoat when touch dry.

2.5	DRYING TIME:		2 to 8 hours, very dependent on the drying conditions.

2.6	COVERAGE:		Theoretical - to 10 sq. Metres per litre.

Practical     - 6 - 10 sq. Metres per litre.

2.7	PACK SIZE:		25 litre or 200 litre drums.

2.8	FLASH POINT:	 	None.

2.9	APPEARANCE:	When properly applied, Enviroguard is invisible on stone, brick and 				other building  materials.

2.10	REMOVAL:		Enviroguard can be removed by pressure washing using water at 				85oC or by using Envirogel followed by cold water.

2.11	THINNERS:		Clean water, only as required up to 20% for first coat or to improve

spray properties

3.	PREPARATION

3.1	Surfaces should be clean and free from surface dirt, dust and grease.

3.2	All loose friable material should be removed and damaged areas made good.

3.3	Efflorescence and laitence should be treated as appropriate.

3.4	Existing mould growth should be treated and removed.

3.5	Where graffitti removal has been carried out, ensure that the area is well rinsed with water to 	remove all traces of oil or solvent.

TECHENVD.DOC Page 2 of

4.	APPLICATION

4.1	Enviroguard as supplied is ready to use.

4.2	Apply Enviroguard when the air and surface temperature is between 5oC and 25oC and the 	relative humidity between 40% and 90%.

4.3	For brush and roller applications, it is important to achieve a smooth, even coating. Do not 	overload brushes and rollers with excessive quantities of product so as to cause runs or 	ponding. Only use brushes or rollers on smooth surfaces.

4.4	After applying by roller, lay off by brush for an even finish. Brushing should not be so 	vigorous as to cause excessive foaming.

4.5	For spray work, apply by airless or air assisted sprayers in evenly applied fine mist coats 	using a maximum tip size of 0.017mm. For back-pack pump sprayers, thin as necessary with 	up to 20% clean water.

4.6	Apply at the recommended coverage rates.,

4.7	On poured concrete or textured surfaces, take care to cover all of the surface irregularities 	and indents. Subsequent removal of graffitti from poorly coated areas may prove difficult.

4.8	After use, all equipment should be cleaned by washing with warm soapy water. Dried product 	can be 	removed using hot water with a trace of household ammonia added.

5.	GRAFFITTI REMOVAL

5.1	Graffitti damage can easily be removed from treated surfaces as follows:

5.2	On heavily contaminated surfaces apply Envirogel or Cleanaway GTi by brush and leave in 	contact 	for 30 - 60 minutes to soften the graffitti.

5.3	Agitate the treated area using a bronze wire brush to help break up the graffitti. After a 	further 30 minutes, wash the surface clean with hot water.

5.4	Repeat the process as necessary.

5.5	Use a hot water pressure washer to clean larger areas from bottom up. Where hot water is 	available, the use of graffitti removers should not be required.

5.6	In both instances, the protective coating is removed along with the graffitti. One or two coats of Enviroguard should be reapplied to cleaned areas when they have dried.

6.	HEALTH AND SAFETY

These products are considered to be non hazardous. However, please ensure that operators 	read and understand the health and safety data sheet before using these materials.

Revised May 2000