TECHNICAL DATA SHEET. 			TECHEVST.DOC Page 1 of 2

1.	IDENTIFICATION OF PRODUCT AND COMPANY

1.1	Product name : 	ENVIROSTEEL

Water based anti-corrosion treatment for rusted steel

1.2	Company        :  D.Adam & Associates / ACTEL Coatings

Clarendon, 17 High Cross Avenue, Melrose TD6 9SQ Scotland, U.K.

Tel: +44  07880 805478

http://www.actel.f9.co.uk/    E-Mail: dougadam@globalnet.co.uk

2.	TECHNICAL DATA

2.1	STORAGE:		Protect from freezing.

2.2	APPLICATION:		Rust Conversion - Apply one coat by stiff brush.

Wet blast inhibitor - add 10 % Envirosteel to final rinse water.

2.3	OVERCOATING:	Allow a minimum of 24 hours when overcoating with solvent based 				materials.

2.4	DRYING TIME:		2 to 4 hours, very dependent on the drying conditions.

Full reaction time 24 hours.

2.5	COVERAGE:		Theoretical  - up to 30 sq. Metres per litre.

Practical      - 20 sq. Metres per litre.

2.6	PACK SIZE:		25 litre or 200 litre drums.

2.7	DRY FILM:		N/A

2.8	FLASH POINT:		None.

2.9	FIRE RESISTANCE:	Tested to Class “0” BS 476 Parts 6 & 7 - Passed

2.10	TOXICITY:		Non toxic. Approved for use in food and drinks manufacturing plants 				by Departments of Agriculture for Canada and The United States.

TECHEVST.DOC Page 2 of 2

3.	PREPARATION

3.1	Envirosteel is supplied ready to use. Stir well before use. DO NOT THIN.

3.2	When using Envirosteel, always decant into a separate container and never return surplus 	material to the original container.

3.3	Surfaces should be clean and free from surface dirt, dust and grease. Light to medium rusted 	steelwork must be properly prepared by wire brush or power tools (SSPC.SP3) to remove 	loose millscale and flaky rust and paint, which is not sound or tightly adhered.

  - Weathered marine steel plate should be high pressure water or wet abrasive blasted to

SSOC-SP6.

3.5	Best results are achieved if some bright metal (10%) is showing in the rusted area.

3.6	Apply Envirosteel when the humidity is greater than 40%.

On warmer days it is recommended to damp down warm steel with a mist of water prior to 	application.

4.	APPLICATION

4.1	Envirosteel should be stored at room temperature (20oC/68oF) for 24 hours before use. Best 	applied by stiff brush or deck scrubber to encourage penetration of rusted surfaces.

Envirosteel can also be applied by spray.

4.2	Envirosteel can be applied at a rate of 10% to the final rinse water in ultra high pressure 	water jetting applications to prevent flash rusting.

4.3	Apply Envirosteel when the air and surface temperatures are between 5oC and 30oC and the 	relative humidity between 40-90%.

4.4	A thin, even coat applied by brush is the preferred method of application.

Brush Envirosteel well into the rust to ensure complete coverage.

4.5	The changing colour of the Envirosteel coating 	indicates that the chemical reaction is taking 	place. After treatment with Envirosteel, the overall area should be navy/black in 	appearance. If this is not the case, insufficient surface preparation has been carried out.

4.6	Envirosteel will normally be touch dry within 2 hours depending on the temperature and 	humidity. Cooler temperatures delay curing. Allow 24 hours before overcoating solvent 	based topcoats.

4.7	Wash brushes and equipment with water immediately after use. Clean spray lines before 	Envirosteel dries.

5.	HEALTH AND SAFETY

These products are considered to be non hazardous. However, please ensure that operators 	read and understand the health and safety data sheet before using these materials.

Revised May 1999