TECHNICAL DATA SHEET. 		TECHfFLYA.DOC Page 1 of 2

1.	IDENTIFICATION OF PRODUCT AND COMPANY

1.1	Product name : 	FLY-AWAY

Non stick coating to prevent fly posting

1.2	Company        :  ACTEL Coatings

Clarendon, 17 High Cross Avenue, Melrose TD6 9SQ, Scotland, U.K.

Tel: +44  1786 472465,  07880 805478

http://www.actel.f9.co.uk   E-Mail: dougadam@globalnet.co.uk

2.	TECHNICAL DATA

2.1	STORAGE:		Protect from naked flames.

2.2	APPLICATION:		For light to moderate protection, apply a minimum of two coats by

spray, brush or roller. For application to metal surfaces, dilute with

White Spirit until brush marks are eliminated (up to 20%).

On porous surfaces, apply one coat of Enviroguard as a primer and

allow to dry thoroughly.

2.3	OVERCOATING:	Recoat when touch dry.

2.4	DRYING TIME:		2 to 8 hours, very dependent on the drying conditions.

2.5	COVERAGE:		Theoretical - to 10 sq. Metres per litre.

Practical     - 6 - 10 sq. Metres per litre.

2.6	PACK SIZE:		5 litre, 25 litre or 200 litre drums.

2.7	FLASH POINT:	 	38oC.

2.8	APPEARANCE:	When properly applied, FLY-AWAY is semi-transparent on stone, 				brick and other building  materials.

2.9	REMOVAL:		FLY-AWAY can be removed by cleaning with an

emulsifiable solvent degreaser and a hot water power wash at 85oC.

TECHfFLYA.DOC Page 2 of 2

3.	PREPARATION

3.1	Surfaces should be clean and free from surface dirt, dust and grease.

3.2	All loose friable material should be removed and damaged areas made good.

3.3	Efflorescence and laitence should be treated as appropriate.

3.4	Existing mould growth should be treated and removed.

3.5	Where graffitti removal has been carried out, ensure that the area is well rinsed with water to 	remove all traces of oil or solvent and allow sufficient drying time before applying FlyAway.

4.	APPLICATION

4.1	FLY-AWAY as supplied is ready to use, but thinning may be necessary on non-porous

surfaces

4.2	Apply FLY-AWAY when the air and surface temperature is between 5oC and 25oC and the 	relative humidity between 40% and 90%.

4.3	For brush and roller applications, it is important to achieve a smooth, even coating. Do not 	overload brushes and rollers with excessive quantities of product so as to cause runs or 	ponding.

4.4	After applying by roller, lay off by brush for an even finish.

4.5	For spray work, apply by airless or air assisted sprayers in evenly applied fine mist coats 	or by back-pack pump sprayer, thinned as necessary with up to 20% white spirit.

4.6	Apply at the recommended coverage rates.,

4.7	Porous surfaces, brick, stone etc. should be pre-treated with one coat of Enviroguard.

  - On poured concrete or textured surfaces, take care to cover all of the surface irregularities and indents. Subsequent removal of graffitti from poorly coated areas may otherwise prove

difficult.

4.9	After use, all equipment should be cleaned by washing with white spirit.

5.	POSTER REMOVAL

  - Posters simply fall off and fly away from treated surfaces as a result of weathering, wind and

rain. Self-adhesive stickers are easily peeled off without soaking or scraping. In dry climates,

posters can be removed much more easily with water and a little detergent and low pressure

power washing. Scraping and vigorous cleaning should be eliminated.

Note:	Enviroguard Flyaway can also be used as an anti-graffitti coating on brick, concrete etc. 	Graffitti removal is carried out using a hot water pressure wash with or without Cleanaway Gti  	graffitti remover.

6.	HEALTH AND SAFETY

  - FlyAway is flammable. Please ensure that operators read and understand the health and

safety data sheet before using this material.

Revised May 1999