TECHNAVY.DOC Page 1 of 2

TECHNICAL DATA SHEET.

1.	IDENTIFICATION OF PRODUCT AND COMPANY

1.1	Product name : 	     NAVY STEEL

Water based rust converter / primer

1.2	Company        :  D. Adam & Associates / ACTEL Coatings

Clarendon, 17 High Cross Avenue, Melrose TD6 9SQ Scotland, U.K.

Tel: +44  (0) 7880 805478  E:  dougadam@globalnet.co.uk    www.actel.f9.co.uk

2.	TECHNICAL DATA

2.1	STORAGE:		Protect from freezing.

2.2	APPLICATION:		Apply one or two coats by spray, brush or roller.

2.3	OVERCOATING:	8 hours if overcoating with a water based product. Allow a minimum 				of 24 hours if overcoating with solvent based materials.

2.4	DRYING TIME:		2 to 4 hours, very dependent on the drying conditions.

Full reaction time 24 hours.

2.5	COVERAGE:		Theoretical  - up to 12 sq. Metres per litre.

Practical      - 10 sq. Metres per litre.

2.6	PACK SIZE:		25 litre or 200 litre drums.

2.7	DRY FILM:		25 microns.

2.8	FLASH POINT:		None.

2.9	FIRE RESISTANCE: 	Tested to Class “O” BS 476 Parts 6 & 7 - Passed

2.10	TOXICITY:		Non toxic. Approved for use in food and drinks manufacturing plants

by Departments of Agriculture for Canada and The United States

TECHNAVY.DOC Page 2 of 2

3.	PREPARATION

3.1	Navy Steel is supplied ready to use. Stir well before use. DO NOT THIN.

3.2	When using Navy Steel, always decant into a separate container and never return 	surplus 	material to the original container.

3.3	Surfaces should be clean and free from surface dirt, dust and grease. Light to medium rusted 	steelwork must be properly prepared by wire brush or power tools (SSPC.SP3) to remove 	loose millscale and flaky rust and paint, which is not sound or tightly adhered.

3.4	Weathered steel should be high pressure water or wet abrasive blasted to SSOC-SP6.

3.5	Best results are achieved if some bright metal (10%) is showing in the rusted area.

3.6	Apply Navy Steel when the humidity is greater than 40%.

3.7	On warmer days it is recommended to damp down warm steel with a mist of water prior to 	application.

4.	APPLICATION

4.1	Navy Steel should be stored at room temperature (20oC/68oF) for 24 hours before use. 	Best applied by brush or deck scrubber to encourage penetration of rusted surfaces, but

Navy Steel can also be applied by spray or roller.

4.2	Apply Navy Steel when the air and surface temperatures are between 5oC and 30oC 		and the relative humidity between 40-90%.

4.3	Thin, even coats applied by brush is the preferred method of application. Brush Blue Steel 	Primer 	well into the rust to leave a dry film thickness of 25-30 microns.

4.4	Navy Steel in the wet state is off white in colour. The changing colour of the coating 	indicates that the chemical reaction is taking place. After treatment with Navy Steel, the 	overall area should be navy/black in appearance. If this is not the case, insufficient surface 	preparation has been carried out.

4.5	Navy Steel will normally be touch dry within 2 hours depending on the temperature and 	humidity. Cooler temperatures delay curing. Allow a minimum of 8 hours before overcoating 	with water based products and 24 hours with solvent based topcoats.

4.6	Wash brushes and equipment with water immediately after use. Clean spray lines before 	Navy Steel dries. Once dry, Navy Steel is difficult to remove. Use an aromatic solvent to 	soften dry brushes or free clogged lines.

5.	HEALTH AND SAFETY

These products are considered to be non hazardous. However, please ensure that operators 	read and understand the health and safety data sheet before using these materials.

Revised May 1999