TECHNICAL DATA SHEET. 			TECHSPWMD.DOC page 1 of 2

1.	IDENTIFICATION OF PRODUCT AND COMPANY

Product name : 	HYDRAWAX

Product type:		Ultra thin, alkali resistant water displacing, corrosion

preventative compound for steelwork exposed to salt water.

Company        :  	D. Adam & Associates / ACTEL Coatings

Clarendon, 17 High Cross Avenue, Melrose TD6 9SQ Scotland, U.K.

# Tel: +44 (0) 7880 805478     www.actel.f9.co.uk     dougadam@globalnet.co.uk

2.	TECHNICAL DATA

2.1	STORAGE:		Store securely in original labelled containers away from strong

oxidising agents, naked flames and sources of ignition.

2.2	APPLICATION:		Apply by spray or dipping

2.3	OVERCOATING:	Do not apply paints to surfaces which have been protected by

HYDRAWAX  without complete removal of the product by solvent

degreasing.

2.4	COVERAGE:		Theoretical  - up to   12 sq. metres per litre.

Practical      - 8 to 12 sq. metres per litre.

2.5	PACK SIZE:		5, and 25 litres and 200 litre drums.

2.6	FLASH POINT:		+ 120oC

2.7	SPECIFICATIONS:	MIL-C-81309 corrosion preventative, w.d., ultra thin film

VVL-L-800-C low temp. general purpose preventative

Ford M14 90 A/B Rust preventative

2.8	FIRE RESISTANCE: 	Does not support combustion after the flame source is removed

2.9	STABILITY:		Normally stable. Avoid strong oxidising agents. Combustion of bulk

product may produce oxides of Carbon, Sulphur, Barium and organic

acids

  - MAJOR PROPERTIES:Natural capillarity with adsorption into the interstices of steel

Water displacement

Transparent films

Alkali resistance

TECHSPWMD.DOC page 2 of 2

3.	PREPARATION

3.1	HYDRAWAX  is supplied ready to use.

3.2	Ensure proper ventilation in confined areas.

4.	APPLICATION

  - HYDRAWAX  is best applied by spray or dipping. HYDRAWAX  can also be applied

by brush.

4.2	Nominal coverage rates of 20m2 per litre are possible on smooth surfaces.

  - Wash equipment with white spirit immediately after use. Clean spray lines before

HYDRAWAX  dries.

5.	HEALTH AND SAFETY

Please ensure that operators read and understand the Health and Safety Data Sheet before

using this material.

Revision dated 20th May ‘03