TECHNICAL DATA SHEET. 		TECHENVG.DOC Page 1 of 2

1.	IDENTIFICATION OF PRODUCT AND COMPANY

1.1	Product name : 	ENVIROGUARD ANTI-GRAFFITTI

Water based heavy duty sacrificial anti-graffitti coating

1.2	Company        :  D. Adam & Associates / ACTEL Coatings

Clarendon, 17 High Cross Avenue, Melrose TD6 9SQ Scotland, U.K.

Tel: +44  (0) 7880 805478  E:  dougadam@globalnet.co.uk    www.actel.f9.co.uk

2.	TECHNICAL DATA

2.1	STORAGE:		Protect from freezing.

2.2	APPLICATION:		Apply one or two coats of Enviroguard Anti-Graffitti by spray, 				brush or roller to surfaces already  primed by one coat of 					Enviroguard.

2.3	OVERCOATING:	Enviroguard Anti-graffitti can be applied in two mist coats, wet on 				wet. Otherwise, recoat when touch dry.

2.4	DRYING TIME:		2 to 8 hours, very dependent on the drying conditions.

2.5	COVERAGE:		Theoretical - to 10 sq. Metres per litre.

Practical     - 6 - 10 sq. Metres per litre.

2.6	PACK SIZE:		25 litre or 200 litre drums.

2.7	FLASH POINT:	 	None.

2.8	APPEARANCE:	When properly applied, Enviroguard Anti-Graffitti is invisible on 				stone, brick and other building  materials.

2.9	REMOVAL:		Enviroguard Anti-Graffitti can be removed by pressure washing 				using water at 85oC or by using Envirogel followed by cold water.

3.	PREPARATION

3.1	Surfaces should be clean and free from surface dirt, dust and grease.

3.2	All loose friable material should be removed and damaged areas made good.

3.3	Efflorescence and laitence should be treated as appropriate.

3.4	Existing mould growth should be treated and removed.

3.5	Where graffitti removal has been carried out, ensure that the area is well rinsed with water to 	remove all traces of oil or solvent.

TECHENVG.DOC Page 2 of 2

4.	APPLICATION

4.1	Enviroguard Anti-Graffitti as supplied is ready to use.

4.2	Apply Enviroguard Anti-Graffitti when the air and surface temperature is between 5oC and 	25oC and the relative humidity between 40% and 90%.

4.3	For brush and roller applications, it is important to achieve a smooth, even coating. Do not 	overload brushes and rollers with excessive quantities of product so as to cause runs or 	ponding.

4.4	After applying by roller, lay off by brush for an even finish. Brushing should not be so 	vigorous as to 	cause excessive foaming.

4.5	For spray work, apply by airless or air assisted sprayers in evenly applied fine mist coats with 	a maximum tip size of 0.017 mm. For back-pack pump sprayers, thin as necessary with up to 	20% clean water.

4.6	Apply at the recommended coverage rates.,

4.7	On poured concrete or textured surfaces, take care to cover all of the surface irregularities 	and indents. Subsequent removal of graffitti from poorly coated areas may prove difficult.

4.8	After use, all equipment should be cleaned by washing with warm soapy water. Dried product 	can be removed using hot water with a trace of household ammonia added.

5.	GRAFFITTI REMOVAL

5.1	Graffitti damage can easily be removed from treated surfaces as follows:

5.2	On heavily contaminated surfaces apply Envirogel or Cleanaway GTi by brush, and  leave 	in contact for 1 hour up to 8 hours depending upon weather conditions to soften the graffitti.

5.3	Agitate the treated area using a bronze wire brush to help break up the graffitti.

5.4	 After a further 1/2 to 1 hour wash the surface clean with hot water.

5.5	Repeat as necessary.

5.6	Use a hot water pressure washer to clean larger areas from the bottom up. Where hot water 	is available, the use of graffitti removers should not be required.

5.7	In both instances, the protective coating is removed along with the graffitti. One coat of 	Enviroguard 	Anti-Graffitti should be reapplied to cleaned areas when they have dried.

6.	HEALTH AND SAFETY

6.1	These products are considered to be non hazardous. However, please ensure that operators 	read and understand the health and safety data sheet before using these materials.

Revised May 1999