TECHNICAL DATA SHEET. 			TECHPROF.DOC page 1 of 2

1.	IDENTIFICATION OF PRODUCT AND COMPANY

Product name:		STEEL PROOF

Product type:		Semi hard anti-corrosion wax coating for ferrous and

non ferrous metals designed to meet MIL-C-16173D-4 for

automotive cavity protection and for protection of steel in

severe salt exposure environments

Company        :  	D. Adam & Associates / ACTEL Coatings

Clarendon, 17 High Cross Avenue, Melrose TD6 9SQ Scotland, U.K.

Tel: 07880 805478

www.actel.f9.co.uk   E-Mail: dougadam@globalnet.co.uk

2.	TECHNICAL DATA

2.1	STORAGE:		Store securely in original labelled containers

away from oxidisers, naked flames and sources of ignition.

2.2	APPLICATION:		Apply by spray, brush or roller at  80. to give 40.  d.f.t

2.3	OVERCOATING:	Do not apply other coating materials or paints to surfaces which 			            have been protected by Steel Proof without complete removal of 				the product by solvent degreasing.

2.4	DRYING TIME:		4 to 6 hours, very dependent on the drying conditions and w.f.t.

2.5	COVERAGE:		Theoretical  - up to 10 sq. metres per litre.

Practical      - 5 to 8 sq. metres per litre.

2.6	PACK SIZE:		5, 25 litres and 200 litre steel drums

2.7	DRY FILM:		40  To give 1000+ hours salt fog resistance per ASTM-B 117

2.8	FLASH POINT:		43oC.

2.9	SPECIFICATION:	Complies with MIL-C-83933A(MR) and MIL-C-62218 for rust 					preventative compounds for steelwork and MIL-C-16173D-4 for

motor vehicle cavity protection

2.10	FIRE RESISTANCE: 	Does not support combustion after the flame source is removed

2.11	FLEXIBILITY:		Coating will not crack, peel or chip when bent 180o around a mandrel 				3/16 inch in diameter which has been cooled to -10oF

2.12	STABILITY:		Normally stable. Keep away from strong oxidising agents. Fire

of bulk wet product creates Carbon Monoxide and Carbon Dioxide

vapours.

2.13	OPERATING TEMPERATURES:	  -50oC to +150oC

2.14	CORROSION TESTS:	Salt fog resistance ASTM-B 117		1100 hours + at 40

Salt water immersion			Passes

Creep penetration after 7 days		Passes

TECHPROF.DOC page 2 of 2

3.	PREPARATION

3.1	Steel Proof is supplied ready to use. Stir well before use. DO NOT THIN.

3.2	Ensure proper ventilation in confined areas.

3.3	Surfaces should be clean and free from surface dirt, dust, grease and any corrosion 	products.

3.4	Weathered steel should be high pressure water or wet abrasive blasted to SSOC-SP6.

3.5	Best results are achieved on rusted areas if they are first passivated by treating with 	Envirosteel or Navy Steel.

4.	APPLICATION

  - Major applications include:

steel structures box sections

preservative film during metal seam welding

auto under-body coatings

heavy duty coatings for steelwork exposed to severe salt weathering

preservative and mould release wax for light weight concrete formwork

  - Steel Proof should preferably be stored at room temperature (20oC/68oF) for 24 hours

before use. Best applied by airless spray. Steel Proof can also be applied by brush or roller.

4.3	Nominal coverage rates of 10m2 per litre are possible on smooth surfaces.

Actual coverage will be determined by the profile of the substrate to be coated and the dry

film thickness specified.

4.4	Steel Proof will normally be touch dry within 4 hours depending on the temperature and 	humidity. Cooler temperatures delay curing.

  - Wash brushes and equipment with white spirit immediately after use. Clean spray lines with

white spirit before Steel Proof dries.

5.	HEALTH AND SAFETY

This product is flammable with a Flash Point of 43oC. Please ensure that operators 	read and understand the Health and Safety Data Sheet before using this material.

Revision dated 20th May ‘03