TECHNICAL DATA SHEET. 			TECHPROF.DOC page 1 of 2

1.	IDENTIFICATION OF PRODUCT AND COMPANY

Product name:		STEEL PROOF TFH

Product type:	Thin film anti-corrosion hard wax coating for dip and

spray protection of ferrous and non ferrous metals and machined

components during medium term outdoor exposure.

Company        :  	D. Adam & Associates / ACTEL Coatings

Clarendon, 17 High Cross Avenue, Melrose TD6 9SQ Scotland, U.K.

Tel: 07880 805478

http://www.actel.f9.co.uk   E-Mail: dougadam@globalnet.co.uk

2.	TECHNICAL DATA

2.1	STORAGE:		Store securely in original labelled containers

away from oxidisers, naked flames and sources of ignition.

2.2	APPLICATION:		Apply by spray or dipping

2.3	OVERCOATING:	Do not apply coating materials or paints other than those in the

Steel Proof range of products, to surfaces which have been protected

by Steel Proof TFH without testing for compatibilty.  Steel Proof

TFH can be removed by solvent washing or abrasive blasting

2.4	DRYING TIME:		60 minutes, very dependent on the drying conditions and w.f.t.

2.5	COVERAGE:		Theoretical  - up to 10 sq. metres per litre.

Practical      - 6 to 10 sq. metres per litre.

2.6	PACK SIZE:		5, 25 litres and 200 litre steel drums

2.7	DRY FILM:		20 from 37 w.f.t to give 400+ hours salt fog resistance per ASTM-

B 117

2.8	FLASH POINT:		43oC.

2.9	FIRE RESISTANCE: 	Does not support combustion after the flame source is removed

2.11	FLEXIBILITY:		Coating will not crack, peel or chip when bent 180o around a mandrel 				3/16 inch in diameter which has been cooled to -10oF

2.12	STABILITY:		Normally stable. Keep bulk product away from strong oxidising

agents

2.13	OPERATING TEMPERATURES:	  -18oC to +50oC

2.14	CORROSION TESTS:	Salt fog resistance ASTM-B 117		400+ hours + at 20

Salt water immersion			Passes

Creep penetration after 7 days		Passes

TECHPROF.DOC page 2 of 2

3.	PREPARATION

3.1	Steel Proof TFH is supplied ready to use. Stir well before use. DO NOT THIN.

3.2	Ensure proper ventilation in confined areas.

3.3	Surfaces should be clean and free from surface dirt, dust, grease and any corrosion 	products.

3.4	Weathered steel should be high pressure water or wet abrasive blasted to SSOC-SP6.

4.	APPLICATION

  - Major applications include:

steel structures box sections

preservative film during metal seam welding

heavy duty coatings for steelwork exposed to severe salt weathering

4.2	Steel Proof TFH should be stored at room temperature (20oC/68oF) for 24 hours before use.

Best applied by airless spray. Steel Proof TFH can also be applied by dipping.

4.3	Nominal coverage rates of 10m2 per litre are possible on smooth surfaces.

Actual coverage will be determined by the profile of the substrate to be coated and the dry

film thickness specified.

4.4	Steel Proof will normally be touch dry within 1 hour depending on the temperature and 	humidity. Cooler temperatures delay drying.

  - Wash equipment with white spirit immediately after use. Clean spray lines with

white spirit before Steel Proof TFH dries.

5.	HEALTH AND SAFETY

This product is flammable with a Flash Point of 43oC. Please ensure that operators 	read and understand the Health and Safety Data Sheet before using this material.

Revision dated 20th May ‘03